HOT STAMPING FOIL HSF49718 Black and White

* **EASY TO USE**
* **MULTI-RECEPTOR COMPATIBILITY**

**HSF49718**

A versatile foil which can be used in many different applications.

Coated on a 12μm PET fi lm.

Coating weight: 8 to 14 g/m2.

Transfer temperature around 100°C.

Possible to print at high speeds.

High versatility, print on papers, PVC, vinyl, PET, PA (nylon), leather, etc.

High coverage abilities with excellent sharpness.

Very good smudge, scratch and abrasion resistance.

**CERTIFICATIONS AND SAFETY DATA**

All MSDS are available on request.

Storage conditions: 12 months in 5–35°C and 20-80% humidity.

HSF49718 complies to EC directives:

• 1935/2004 EC (food contact),

• 1994/62/EC (packaging and waste),

• 1998/638/EC (heavy metals),

• 1999/45/EC and 2001/59/EC (dangerous substances),

• 2000/53/EC (ELV),

• 2002/95/EC (RoHs),

• 2002/96/EC (WEEE),

• REACH: as a European manufacturer, TYPERITE is completely

fulfi lling REACH requirements. Our foils are free from the

Substances of Very High Concern (SVHC).